## Slide 1: A Summary of my Research at ASU
Sagnik Dasgupta
08/13/2020

## Slide 2: Transparent, passivating, and carrier-selective contacts to silicon solar cells
Carrier selective contacts on tunnel oxide
  SiO2/Poly-Si – NREL Baseline
  SiO2/ITO – Young et. al, PVSC-2014
    50Å SiO2
Two Key Challenges:
  Passivation
  Contact resistivity
p poly
SiOx (1. 5nm)
Si
SiOx (1.5 nm)
n poly
p poly
SiOx (1. 5nm)
Si
SiOx (1.5 nm)
ITO

## Slide 3: Challenges in Experimental realization - Passivation
FGA 350 C 10 min
SiO2 is the passivation layer
2 necessities for effective passivation*
  Hydrogen radicals for dangling bonds
  Capping layer on oxide
PECVD aSi:H capping layer and hydrogen source
Hydrogen overpressure in forming gas promotes diffusion into SiO2 layer
aSi:H stripped by dilute KOH etch
*Mazzarella, L. et al. Optimization of PECVD process for ultra-thin tunnel SiO x film as passivation layer for silicon heterojunction solar cells. 2017 IEEE 44th Photovolt. Spec. Conf. PVSC 2017 1–5 (2017). doi:10.1109/PVSC.2017.8366698

## Slide 4: Challenges in Experimental realization – Contact Resistivity
Thicker oxides  Better passivation  Exponentially worse
NREL demonstrated with 5 nm SiO2  Too thick for tunneling?
TLM test structures
  2 nm SiO2 + 30 nm ITO
As is  too high for measurement
600 C Anneal  Measurable resistance, but not ohmic
From Fowler-Nordheim tunneling
ITO
Si
SiOx
ITO reacting with SiOx ?
Effective thickness reduced
To do: EDX
Si
SiOx
ITO
ITO

## Slide 5: Simulation of TOPCON cells in AFORS-HET
Reference TOPCON model in AFORS-HET v2.51
Goal: Model device similar to NREL baseline
Defects in cSi/SiOx interface
  1 Å transition layer
  defect density at midgap2
Tunneling Barrier Height of Oxide
  Lower than expected from band alignment3
  Adjusted and to get barrier height 2.5 eV
Results (1.2 nm oxide):
Conclusions:
  Fairly realistic representation of NREL’s baseline
  Reference for comparing to devices with novel contacts
1. Varache, R. et al. Investigation of selective junctions using a newly developed tunnel current model for solar cell applications. Sol. Energy Mater. Sol. Cells 141, 14–23 (2015).
2. King, T. J., Hack, M. G. & Wu, I. W. Effective density-of-states distributions for accurate modeling of polycrystalline-silicon thin-film transistors. J. Appl. Phys. 75, 908–913 (1994).
3. Gan, J.-Y. Polysilicon emitters for silicon concentrator solar cells. (Stanford University, 1990).

## Slide 6: Partial Specific Contact Resistances as a Proxy for Device performance
Simulations in PC1D, Analyzed in MATLAB
Goal:
  Obtain electron and hole partial contact resistances
  Function of iV
  From iJV and JV
Simulation assumptions
  Ideal electron contact
  Uniform generation in the absorber
PC1D data
(J-iV; J-V)
Solve for & (2e-2v)
Compare with calculated resistances

## Slide 7: Calculating the partial Specific Contact resistances
Generation current
Radiative recombination
Auger recombination
Shockley-Read-Hall recombination